Table 1:   Electrochemical impedance parameters for blank, mild steel coated with hybrid sol-gel and coated mild steel containing varying doping concentrations of caffeine in 3.5 wt.% NaCl at 303 K.

| Nature of the mild steel substrate | Rs/Ω cm2 | Rcoat/Ω cm2 | CPEcoat/ μF cm-2 | m | Rct/Ω cm2 | CPEdl/ μF cm-2 | n | % IE |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Blank (untreated) | 27.68 | - | - | - | 981.25 | 5903 | 0.6362 | - |
| Hybrid sol-gel coated | 24.71 | 178.25 | 6432 | 0 .7502 | 1954.95 | 4427 | 0.6912 | 49.81 |
| Hybrid sol-gel + 25ppm caffeine | 26.35 | 287.87 | 6377 | 0.6131 | 2441.65 | 2526 | 0.7249 | 59.80 |
| Hybrid sol-gel + 50 ppm caffeine | 28.35 | 329.91 | 2513 | 0.7058 | 2934.94 | 2225 | 0.7338 | 66.57 |
| Hybrid sol-gel + 75 ppm caffeine | 25.81 | 341.54 | 2160 | 0.7667 | 3726.41 | 1538 | 0.7904 | 73.67 |
| Hybrid sol-gel + 100 ppm caffeine | 27.78 | 576.24 | 1540 | 0.7456 | 6218.02 | 1250 | 0.8610 | 84.22 |

Table 2:  Potentiodynamic polarization parameters for blank, mild steel coated with hybrid sol-gel and coated mild steel containing varying doping concentrations of caffeine in 3.5 wt.% NaCl at 303 K.

| Nature of the mild steel substrate | Ecorr/mV | icorr/μA cm-2 | βa/ mV dec-1 | -βc/ mV dec-1 | CR/mpy | % IE |
| --- | --- | --- | --- | --- | --- | --- |
| Blank (untreated) | -658 | 6.3096 | 35 | 38 | 2.91 | - |
| Hybrid sol-gel | -756 | 3.1623 | 82 | 112 | 1.46 | 49.88 |
| Hybrid sol-gel + 25 ppm caffeine | -615 | 2.5119 | 57 | 92 | 1.16 | 60.19 |
| Hybrid sol-gel + 50 ppm caffeine | -577 | 1.9953 | 69 | 77 | 0.92 | 68.38 |
| Hybrid sol-gel + 75 ppm caffeine | -737 | 1.5849 | 45 | 58 | 0.73 | 74.88 |
| Hybrid sol-gel +100 ppm caffeine | -676 | 0.7079 | 79 | 88 | 0.33 | 88.79 |

Table 3: Noise resistance parameters for blank and 100 ppm caffeine doped hybrid sol-gel  coated mild steel specimens in 3.5 wt.% NaCl at 303 K.

| Nature of the mild steel plate | Rn /Ω cm2 | % IE |
| --- | --- | --- |
| Blank (untreated) | 229.73 | - |
| Hybrid sol-gel + 100 ppm caffeine | 1833.69 | 87.47 |

Table 4:  IR bands corresponding to the hybrid sol-gel matrix and the bond formed between the coating and mild steel surface.

| Bond type | Observed peak assignment/ cm-1 | Possible wavelength ranges for relevant peaks/ cm-1 [25] |
| --- | --- | --- |
| Si-O stretching | 1041,1087 | 1000-1130 |
| Si-C bending | 1272, 788 | 1245-1275, 750-865 |
| C-H stretching | 2978 | 2840-3000 |
| C-H bending | 1453 | 1300-1500 |
| O-H stretching | 3301 | 3200-3600 |
| NH2 bending | 1635 | 1600-1650 |
| Fe-O-Si vibrations and Si-O-H stretching | 954 | 968 |

Table 5: Elemental compositions (wt.%) of bare mild steel, blank mild steel, and caffeine   doped silane coatings on mild steel acquired using EDX analysis.

| Nature of the mild steel specimen |  | Elemental composition (wt.%) Fe O C Si Cl |
| --- | --- | --- |
| Bare |  | 96.15 3.24 0.61 - - |
| Blank (untreated) |  | 54.33 35.96 9.11 - 0.60 |
| Hybrid sol-gel + 100 ppm caffeine |  | 85.44 7.52 2.56 4.36 0.12 |